## Slide 1: Vistec #2
Alignment
PEC (Proximity Effect Correction)
Undercut with 100 kV

## Slide 2
Alignment marks 20 x 20 µm
Joy marker
Alignment (works :c)

## Slide 3
Alignment marks 20 x 20 µm
Alignment
Kiitos Anna!

## Slide 4
Alignment marks 20 x 20 µm
One premarker
Rotation of wafer with optical microscope
10 nm over full wafer
Additional: marker for each structure
Alignment (works :c) )
Kiitos Emma!

## Slide 5
Alignment marks 20 x 20 µm
Alignment (works :c) )
Kiitos Emma!

## Slide 6
Alignment marks 20 x 20 µm, spacing 3 mm
Alignment (works :c) )
Kiitos Emma!

## Slide 7
Only PEC,
not dose (size)?!!
PEC (Proximity Effect Correction) 90k€ = 10 Lupitos

## Slide 8
Only PEC,
not dose (size)?!!
PEC (Proximity Effect Correction)

## Slide 9
Only PEC,
not dose (size)?!!
Oops, it works?!!??
PEC (Proximity Effect Correction)

## Slide 10
Undercut with 100 kV/dosetest
1000µC/cm2
1200µC/cm2
1400µC/cm2
1800µC/cm2
2000µC/cm2
Kiitos Klaara!

## Slide 11
Undercut with 100 kV/dosetest
2000µC/cm2
Kiitos Klaara!

## Slide 12
Undercut with 100 kV/dose 2000µC/cm2 MIBK 20s Methanol:Methylglycol 2:1
No MG
10s MG
20s MG
30s MG
Kiitos Klaara!

## Slide 13
Undercut with 100 kV/dosetest
30s Methanol:Methylglycol 2:1
Kiitos Klaara!
1000µC/cm2
1305µC/cm2
1513µC/cm2
1650µC/cm2
1916µC/cm2

## Slide 14: Vistec #2
Alignment
PEC (Proximity Effect Correction)
Undercut with 100 kV